No. 2095 GameBoard

Table top GameBoard shall be TimberForm® model No. 2095 in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

GameBoard panel shall be 18 gauge steel measuring 18 inches square.  The panel shall have a porcelain enamel coating depicting red-on-blue graphic of alternating 64-square checkered pattern.  Game pieces are not included.  If attached to a TimberForm table, stainless steel tamper-resistant fasteners with cushioned grommets shall be provided in sufficient quantity to attach the GameBoard to the table surface.

2.  Construction

Four corners of the GameBoard panel shall be rounded to a radius of one inch and all edges smoothly deburred.  The perimeter of the panel shall include eight 1/4 inch diameter holes to accommodate fasteners.

3.  Finish

GameBoard shall be encapsulated with porcelain enamel.  The porcelain enamel process shall fuse a layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, special glasses shall be employed possessing thermal expansion qualities slightly lower than those of the steel substrate.  Colors shall be permanent and extremely weather-resistant.