No. 2115 Skyline Seat with Armrests

Seat shall be TimberForm® Skyline( series model No. 2115, with armrests, in the length and color finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Seat frames shall be cast iron, cast in accordance with ASTM, Specification A48-82, Class 30.  Center support strap shall be 2 inch wide x 1/4 inch thick formed mild steel strap.  All wood shall be clear, kiln dried, Alaska yellow cedar, precision milled to pattern, dressed to a smooth finish, with eased edges and ends, individually selected for quality and appearance.

2.  Construction

Seat frames shall have all parting lines and flask marks ground smooth after casting.  Stretcher pipe and center support strap shall be deburred and ground smooth.  Seat slats shall be attached to cast iron frames and center support strap with No. 10 x 1-1/4 inch stainless steel pan head screws.

3.  Finish

Steel and cast iron parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.