No. 2196 TimberForm Metal Bollard

Bollard shall be TimberForm® model No. 2196 in the color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Bollard post shall be 4 inch i.d. schedule 40 mild steel pipe with a minimum wall thickness of 7/32 inch.  Thin wall tube is not acceptable.  Top of bollard post shall be fitted with a cast aluminum hemi-dome end cap, permanently adhered in place.  Easily vandalized friction fit end caps are not permitted.  Two hardened steel No. 2 pad eyes shall be welded to the post, 180 degrees to one another, with the welds ground smooth.

Mounting shall be –E embedment (permanent), -P pedestal (fixed surface) or –R removable.  Embedment option shall include two 9/16 inch diameter thru holes for No. 4 re-bar (by others).  Pedestal option mounting base shall include 3-7/8 inch o.d. mild steel tube welded to 1/4 inch mild steel plate and a matching decorative base cover to conceal anchors (by others).  Removable option in-ground sleeve shall be 4-inch i.d. schedule 40 mild steel seamless pipe and bollard insert shall be 3-7/8 inch o.d. mild steel tube.  Removable bollard post and in-ground sleeve shall have interlocking tabs for padlock (by others).

2.  Construction

Bollard post shall be a single unit.  Final product shall be free of burrs.

3.  Finish

Steel and cast iron parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.