No. 2199-01 Metal Bollard with Ball Top

Bollard shall be TimberForm® No. 2199-01 in the color finish and mounting style selected by the owner's representative and in the quantity shown on the bills of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

1. Materials

Bollard post shall be 4 inch i.d. schedule 40 mild steel seamless pipe with a minimum wall thickness of 7/32 inch.  Thin wall tube is not acceptable.  Top of bollard post shall be fitted with a 6½ inch dia. cast iron sphere.  Bollard post shall also be fitted with two decorative cast iron rings with a semi-circular cross section.  Hardened steel No. 2 pad eyes welded to post are optional.

Mounting shall be –E embedment (permanent), -P pedestal (fixed surface) or –R removable.  Embedment option shall include two 9/16 inch diameter thru holes for No. 4 re-bar (by others).  Pedestal option mounting base shall include 3-7/8 inch o.d. mild steel tube welded to 1/4 inch mild steel plate.  Removable option in-ground sleeve shall be 4-inch i.d. schedule 40 mild steel seamless pipe and bollard insert shall be 3-7/8 inch o.d. mild steel tube.  Removable bollard post and in-ground sleeve shall have interlocking tabs for padlock (by others).

2.  Construction

Bollard post, sphere and decorative rings shall be permanently and continuously welded into a single unit.  Final product shall be free of burrs.

3.  Finish

Bollard shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.