No. 2218-16 Colossus Big Timber Seat

Seat shall be TimberForm® Colossus( series model No. 2218-16, sixteen feet long, in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Timber shall be free-of-heart-center (F.O.H.C) coastal Douglas fir, fine-grained.  There shall be no loose knots, knotholes, shake, unsound wood, whitespeck or honeycomb allowed.  Timbers shall be nominal 8 inch x 12 inch. To eliminate slivering, timbers shall be free of wane, and planer skips are not allowed in dressing.  Except as noted, other characteristics and limiting provisions are in accordance with Paragraph 131-A Standard Grading Rules for West Coast Lumber.

2.  Construction

Seat shall ship unassembled and include installation hardware for assembly by contractor.  Each support leg shall be assembled and welded into a single unit. Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.  Seats shall attach to frame with 5/8 inch x 8 inch hot-dipped galvanized lag screws.

3.  Finish

Timber shall be preservatively treated with a non-toxic formulation capable of deep penetration without materially changing the color of the wood to which it is applied.

Support legs shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.