No. 2627-6 Broadway Bench with Intermediate Armrest

Bench shall be TimberForm® Broadway( series model No. 2627-6 six feet long, with intermediate armrest, in the color finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Frames including armrests and legs shall be fabricated from smooth 1/2 inch thick mild steel bar with edges uniformly eased (rounded).  Slat support straps and intermediate armrest supports shall be 1/4 curved steel bars permanently welded to top and bottom rails. Intermediate armrest shall be permanently welded to the bottom rail and front-facing armrest support. All ends and edges will be rounded. Top and bottom rails shall be 1 inch i.d. schedule 40 mild steel pipe.  Thin wall tubing shall not be permitted. All wood shall be clear, kiln dried, Alaska yellow cedar, precision milled to pattern, dressed to a smooth finish with eased edges and ends, individually selected for quality and appearance.

2.  Construction

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs. Bench slats shall be attached to support straps with two piece 1/4 inch diameter Cherrymate aluminum rivets.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.