No. 2674 Metro Picnic Table with Seats

Picnic Table with Seats shall be TimberForm® Metro( series model No. 2609, 6’ in length, in the color finish as selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, www.timberform.com. Phone 800/547-1940.

1.  Materials

Seat and tabletop shall be 12 gauge formed perforated mild steel plate; perforation shall be a dot dash pattern.  Seat and table frame shall be fabricated from schedule 40 mild steel tube and .25-inch-thick steel plate.  Mounting shall be -P pedestal (surface) mount.

2.  Construction

Each seat and tabletop shall be assembled and welded into separate units and shall attach to table frame with stainless steel hardware.  Welds shall be smooth and continuous with no gaps or pin holes.  The final product shall be free of weld spatters and burrs.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.