No. 2802 Renaissance Seat with Armrests

Seat shall be TimberForm® Renaissance( series model No. 2802, with armrests, in the length and color finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Frames including armrests and legs shall be fabricated from 1 inch x 1 inch square mild steel bar.  Seat basket shall include .188 inch thick x 1-1/2 inch wide formed mild steel strap with 1 inch i.d. schedule 40 mild steel seamless pipe and 3/8 inch x 3/8 inch mild steel bar.  Legs shall include 5/8 inch diameter holes for anchor bolts (by others).

2.  Construction

Right and left frames and the seat basket shall be assembled and welded into separate units.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.  Assembly hardware shall be stainless steel.

3.  Finish

Steel and cast iron parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.