No. 2013 Diller Seat with Armrests

Seat shall be TimberForm® Diller( series model No. 2013, in the length, color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

- Materials

Frames shall be fabricated from 3/8 inch thick bent steel plate.  Mounting shall be surface style for permanent or moveable applicaitons.

Slats shall be free-of-heart-center, kiln-dried, premium Douglas fir.  There shall be no loose knots nor knotholes. To eliminate slivering, wood shall be free of wane, smoothly dressed four sides. Seat and backrest shall be nominal size of 3 inch x 6 inch and have their edges and ends heavily eased.  Armrests shall be nominal 3 inch by 4 inch and have their edges and ends heavily eased. After fabrication, timber shall be preservatively treated with a non-toxic formulation capable of deep penetration without materially changing the color of the wood to which it is applied.

- Construction

Slats with No. 14 x 2 inch stainless steel pan head screws.

- Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.