No. 2186-4 Rectangular Metal Sign

Metal Sign shall be TimberForm® model No. 2186-4, in the color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Frame shall be fabricated from 4 inch i.d. schedule 40 mild steel seamless pipe.  Sign panel shall be 3/16" thick mild steel plate and shall include three collar inserts.  Sign panel shall connect to frame with three cast aluminum (384 alloy) two-piece attachment collars.  Collars must be formed to recess bolt fastener.  Each collar set shall include two vandal-resistant socket-head cap screws with nuts and two 1/4" aluminum hammer-drive rivets.  Mounting shall be -P pedestal (fixed leveling) or -E embedded (permanent) as selected by the owner's representative.  A matching decorative base cover shall conceal mounting hardware on –P option.

2.  Construction

Frame shall be one-piece construction.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3.  Finish

Steel parts shall be coated with CASPAX-7, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.