No. 2669-12 Craftsmen Rectangular Planter

Planter shall be TimberForm® Craftsmen® series model No. 2669-12 in the color finish selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Planter shall be cast iron conforming to ASTM Specification A48-82, Class 30.  Planter sides shall include a chrysanthemum graphic as standard with rhododendron and custom graphics available upon request.  Each frame shall also accommodate optional raised lettering available in a variety of letter styles. Top and bottom connection plates shall be fabricated from .25-inch (1/4”) thick mild steel.

2.  Construction

Frames shall have all parting lines and flask marks manually ground smooth after casting. Installing contractor shall assemble the frames and connection plates into a single unit.

3.  Finish

All parts shall be coated with CASPAX-7, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.