No. 2977-3 Renaissance Accessible Integral Table with Three Seats

Accessible Integral Table with Three Seats shall be TimberForm® Renaissance( series model No. 2977-3 in the color selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Table top shall be 43-3/4 inch diameter with perimeter constructed of formed 1 inch i.d. schedule 40 mild steel seamless pipe.  Table surface shall be fabricated from .188 inch thick x 1-1/2 inch wide mild steel flat bar.  Table top connection bracket shall be fabricated from 1/4 inch steel plate. Seat shall consist of smooth .188 inch thick x 1-1/2 inch wide formed mild steel strap whose edges are uniformly eased, 1 inch i.d. schedule 40 mild steel seamless pipe, and 3/8 inch x 3/8 inch mild steel bar.

Upper and lower connection rings shall be fabricated from 4 inch i.d. schedule 40 steel pipe.  Support legs are fabricated from 2 inch i.d. schedule 40 steel pipe. All assembly hardware shall be stainless steel.  Separate leveling hardware shall be fitted with non-marring UHMW pads.

2.  Construction

Table frame and seat shall be welded into a one piece unit.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.