No. 2982 Bistro Tall Seat

Tall Seat shall be TimberForm® Bistro( series model No. 2982-01 or 2982-02, in the seat style and color finish selected by the owners representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

1.  Materials

Post shall be fabricated from 3-1/2 inch i.d. schedule 40 mild steel seamless pipe.  Seat frame shall be fabricated from 1 inch i.d. schedule 40 mild steel seamless pipe.  3/16 inch thick bent steel plate welded to the post shall be used for attachment of seat top.  Three 5/8 inch diameter holes shall be provided for embedded anchoring bolts (by others).

No. 2892-01 seating surface shall be lead-free SofDek thermoplastic coated 12 gauge perforated steel with 7/16” diameter holes.

No. 2892-02 seating surface shall be shall 1 inch x 1 inch x 1/8 inch welded wire grid.

2.  Construction

Seat post and seat top shall be assembled and welded into a two separate units.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.  Stainless steel hardware shall be used to attach seat top to post.

3.  Finish

Steel parts shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.